DIVISION 9 - FINISHES

SECTION 099600 – HIGH PERFORMANCE RESINOUS WALL COATINGS

- GENERAL

      - SUMMARY

        - This Section includes:

          - High-performance resinous wall and ceiling coating systems.

      - SUBMITTALS

        - Product Data:  For each type of product indicated.

        - Installer Certificates for Qualification: Signed by manufacturer stating that installers comply with specified requirements.

        - Material Certificates:  For each resinous wall and ceiling component, from manufacturer.

        - Maintenance Data: For maintenance manuals.

        - Samples: Submit two 6” X 6” samples of each resinous wall and ceiling system applied to a rigid backing.  Provide sample which is a true representation of proposed field applied finish.  Provide sample color and texture for approval from Owner in writing or approved by General Contractor prior to installation.

        - Product Schedule: For resinous wall and ceiling coating systems.

      - QUALITY ASSURANCE

        - Installer Qualifications: Manufacturer's authorized representative who is trained and approved for installation of wall and ceiling systems required for this Project.

          - Engage an installer who is approved in writing by resinous wall and ceiling manufacturer as qualified to apply resinous wall and ceiling systems indicated.

          - Installer Letter of Qualification: Installer to provide letter stating that they have been in business for at least 5 years and listing 5 projects in the last 2 years of similar scope. For each project provide: project name, location, date of installation, contact information, size of project, and manufacturer of materials with system information.

        - Source Limitations:  Obtain primary resinous wall and ceiling materials, including primers, resins, hardening agents, grouting coats, and topcoats, from single source from single manufacturer.  Provide secondary materials, including patching and fill material, joint sealant, and repair materials, of type and from source recommended by manufacturer of primary materials.

        - Pre-installation Conference: Conduct conference at Project site before work and mockups begin.

        - Mockups:  Apply mockups to verify selections made under sample submittals and to demonstrate aesthetic effects and set quality standards for materials and execution. Do not cover up mockup area.

          - Apply full-thickness mockups on 16 square foot floor area selected by Architect.

          - Finish surfaces for verification of products, color, texture, and sheen.

          - Simulate finished lighting conditions for Architect's review of mockups.

          - Approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

          - Mockup shall demonstrate desired slip resistance for review and approval by Owner’s representative in writing.

      - DELIVERY, STORAGE, AND HANDLING

        - Deliver materials in original packages and containers, with seals unbroken, bearing manufacturer's labels indicating brand name and directions for storage and mixing with other components.

          - Maintain containers in clean condition, free of foreign materials and residue.

          - Remove rags and waste from storage areas daily.

      - PROJECT CONDITIONS

        - Environmental Limitations:  Comply with resinous wall and ceiling manufacturer's written instructions for substrate temperature, ambient temperature, moisture, ventilation, and other conditions affecting resinous wall and ceiling application.

        - Lighting:  Provide permanent lighting or, if permanent lighting is not in place, simulate permanent lighting conditions during resinous flooring application.

        - Close spaces to traffic during resinous flooring application and for not less than 24 hours after application unless manufacturer recommends a longer period.

- PRODUCTS

      - MANUFACTURERS

        - Manufacturers:  Subject to compliance with requirements, provide products by:

          - The Sherwin Williams Company, Cleveland, OH. Representative Contact: Michael Starner (484) 624-2360 michael.starner@sherwin.com .

        - ResuWall Deco Flake

          - Optional Pre-Primer for Ceramic Tile: Resuprime VP 5531 at 750 sq. ft. per gallon.

          - Primer: Resuflor Aqua 3479 at 300-350 sq. ft. per gallon.

          - Body Coat (2 Coats): ResuFloor 3552W at 100-200 sq. ft. per gallon.

          - First Finish Coat: Resuflor Aqua 3479 at 300-350 sq. ft. per gallon

          - Final Finish Coat: Resutile 4685W at 400-500 sq. ft. per gallon

      - MATERIALS

        - VOC Content of Resinous Wall and Ceiling Coating:  Provide resinous wall and ceiling systems, for use inside the weatherproofing system, that comply with the following limits for VOC content when calculated according to 40 CFR 59, Subpart D (EPA Method 24)].

          - Resinous Flooring: 100 g/L.

      - HIGH-PERFORMANCE RESINOUS WALL AND CEILING COATING SYSTEM

        - Resinous Wall and Ceiling Coating:  Abrasion-, impact- and chemical-resistant, high-performance, resin-based, monolithic floor surfacing designed to produce a seamless floor.

        - System Characteristics:

          - Color and Pattern: As indicated from manufacturers listed above.

          - Slip Resistance:  Provide smooth, orange peel finish unless otherwise specified.

- EXECUTION

      - PREPARATION

        - Inspection: Prior to commencing Work, thoroughly examine all underlying and adjoining work, surfaces and conditions upon which Work is in any way dependent for perfect results. Report all conditions which affect Work. No "waiver of responsibility" for incomplete, inadequate or defective underlaying and adjoining work, surfaces and conditions will be considered, unless notice of such unsatisfactory conditions has been filed and agreed to in writing before Work begins. Commencement of Work constitutes acceptance of surfaces.

        - Surface Preparation: Remove all surface contamination, loose or weakly adherent particles, laitance, grease, oil, curing compounds, paint, dust and debris by blast track method or approved mechanical means (acid etch not allowed).  If surface is questionable try a test patch.  Create a minimum surface profile for the system specified in accordance with the methods described in ICRI No. 03732 to achieve profile numbers as follows:

        - CONCRETE SURFACE PROFILE (CSP)

          - Thin film, to 10 mils 						CSP-1 to CSP-3

          - Thin and medium films, 10 to 40 mils		CSP-3 to CSP-5

          - Self-leveling mortars, to 3/16”		              CSP-4 to CSP-6

          - Mortars and laminates, to 1/4” or more		CSP-5 to CSP-10

        - Verify that concrete substrates are dry and moisture-vapor emissions are within acceptable levels according to manufacturer's written instructions.

          - Moisture Testing: Perform tests indicated below.

            - Calcium Chloride Test: Perform anhydrous calcium chloride test per ASTM F 1869. Proceed with installation only after substrates have maximum moisture-vapor-emission rate of 3 lb of water/1000 sq. ft. in 24 hours. Perform tests so that each test area does not exceed 1000 sq. ft. and perform 3 tests for the first 1000 sq. ft.  and one additional test for every additional 1000 sq ft.

            - In-Situ Probe Test: Perform relative-humidity test using in-situ probes per ASTM F 2170. Proceed with installation only after substrates have a maximum 75 percent relative-humidity-level measurement.

      - ENVIRONMENTAL CONDITIONS

        - All applicators and all other personnel in the area of the RF installation shall take all required and necessary safety precautions. All manufacturers’ installation instructions shall be implicitly instructions shall be implicitly followed.

        - Repair damaged and deteriorated concrete according to resinous wall and ceiling manufacturer's written instructions.

        - Alkalinity and Adhesion Testing:  Verify that concrete substrates have pH within acceptable range.  Perform tests recommended by manufacturer.  Proceed with application only after substrates pass testing.

        - Resinous Materials: Mix components and prepare materials according to resinous wall and ceiling manufacturer's written instructions.

        - Use patching and fill material to fill holes and depressions in substrates according to manufacturer's written instructions.

        - Treat control joints and other nonmoving substrate cracks to prevent cracks from reflecting through resinous wall and ceiling according to manufacturer's written instructions.

      - APPLICATIONS

        - Install resinous wall and ceiling coating system over properly prepared concrete surface in strict accordance with the manufacturer's directions.

          - Install the primer and/or base coats over thoroughly cleaned and prepared concrete.

          - Install topcoat over wall and ceiling coating system after excess aggregate or sand dust has been removed.

          - Maintain a slab temperature of 60°F to 80°F for 24 hours minimum before applying wall and ceiling coatings, or as instructed by manufacturer.

        - Apply components of resinous wall and ceiling system according to manufacturer's written instructions to produce a uniform, monolithic wearing surface of thickness indicated.

          - Coordinate application of components to provide optimum adhesion of resinous wall and ceiling system to substrate, and optimum intercoat adhesion.

          - Cure resinous wall and ceiling components according to manufacturer's written instructions.  Prevent contamination during application and curing processes.

          - At substrate expansion and isolation joints, comply with resinous wall and ceiling manufacturer's written instructions.

        - Sealant: Saw cut resinous wall and ceiling topping at expansion joints in concrete slab.  Fill sawcuts with sealant prior to final seal coat application. Follow manufacturer’s written recommendations.

        - Apply primer over prepared substrate at manufacturer's recommended spreading rate.

        - Sand between coats and remove sand dust prior to next coat.

        - Apply topcoats in number indicated for wall and ceiling system and at spreading rates recommended in writing by manufacturer.

      - COMPLETED WORK

        - Cleaning: Upon completion of the Work, clean up and remove from the premises surplus materials, tools, appliances, empty cans, cartons and rubbish resulting from the Work. Clean off all spattering and drippings, and all resulting stains.

        - Protection: Protect Work in accordance with manufacturer's directions from damage and wear during the remainder of the construction period.  Use protective methods and materials, including temporary covering, recommended in writing by resinous flooring manufacturer.

        - Contractor shall insure that coating is protected from any traffic until it is fully cured to the satisfaction of the coating manufacturer.

END OF SECTION 096723