SECTION 09 96 56-EPOXY COATING

**RESUWALL VC EPOXY COATING (40 mils) with URETHANE TOPCOAT**

PART 1 – GENERAL

1.1 RELATED DOCUMENTS

 A. Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 1 Specification Sections, apply to this Section.

1.2 SUMMARY

1. This section includes the following:
2. Epoxy wall coating system as shown on the drawings and in schedules.
3. Related sections include the following:

1. Concrete Curing, section 03 39 00

2. Unit Masonry, section 04 20 00

3. Plaster and Gypsum Board, section 09 20 00

1.3 SYSTEM DESCRIPTION

1. The work shall consist of preparation of the substrate, the furnishing and application of a epoxy based wall coating system, with decorative colored chips and urethane topcoat. The system shall have the color and texture as specified by the Owner with a nominal thickness of 40 mils. It shall be applied to the prepared area(s) as defined in the plans strictly in accordance with the Manufacturer's recommendations.

1.4 SUBMITTALS

1. Product Data: Latest edition of Manufacturer's literature including performance data and installation procedures.
2. Manufacturer’s Safety Data Sheet (SDS) for each product being used.
3. Samples: A 3 x 3 inch square sample of the proposed system. Color, texture, and thickness shall be representative of overall appearance of finished system subject to normal tolerances.
4. Mock-up: provide 4’x4’ to be approved in writing by owner.

1.5 QUALITY ASSURANCE

 A. The Manufacturer shall have a minimum of 10 years experience in the production, sales, and technical

 support of epoxy industrial wall coating, urethanes and related materials.

B. The Applicator shall have been approved by the system manufacturer in all phases of surface preparation and application of the product specified.

 C. No requests for substitutions shall be considered that would change the generic type of the specified System.

 D. System shall be in compliance with requirements of United States Department of Agriculture (USDA),

 Food, Drug Administration (FDA), and local Health Department.

E. A pre-installation conference shall be held between Applicator, General Contractor and the Owner to review and clarification of this specification, application procedure, quality control, inspection and acceptance criteria and production schedule.

 F. System shall be in compliance with the Indoor Air Quality requirements of California Section 01350 as verified

 by a qualified independent testing laboratory.

* 1. PRODUCT DELIVERY, STORAGE, AND HANDLING
1. Packing and Shipping
2. All components of the system shall be delivered to the site in the Manufacturer's packaging, clearly identified with the product type and batch number.

 B. Storage and Protection

 1. The Applicator shall be provided with a storage area for all components. The area shall be between 60 F and 90 F, dry, out of direct sunlight and in accordance with the Manufacturer's recommendations and relevant health and safety regulations.

 2. Copies of Safety Data Sheets (SDS) for all components shall be kept on site for review by the Engineer or other personnel.

 C. Waste Disposal

 1. The Applicator shall be provided with adequate disposal facilities for non-hazardous waste generated during installation of the system.

1.7 PROJECT CONDITIONS

1. Site Requirements
2. Application may proceed while air, material and substrate temperatures are between 60 F and 90 F providing the substrate temperature is above the dew point. Outside of this range, the Manufacturer shall be consulted.
3. The relative humidity in the specific location of the application shall be less than 80 % and the surface temperature shall be at least 5 F above the dew point.
4. The Applicator shall ensure that adequate ventilation is available for the work area.
5. The Applicator shall be supplied with adequate lighting equal to the final lighting level during the preparation and installation of the system.

 B. Conditions of substrate to be coated with epoxy material.

 1. Concrete shall be cured for a minimum of twenty eight days prior to the application of the coating system.

 2. Block wall mortar joints have cured no less than 7 days under good conditions.

 3. Sealers and curing agents should not to be used.

 4. Drywall shall be completely clean and free of any oils, soap residue, and gypsum dust and prepared to a #4 to #5 finish.

 C. Safety Requirements

 1. All open flames and spark-producing equipment shall be removed from the work area prior to commencement of application.

1. "No Smoking" signs shall be posted at the entrances to the work area.

 3. The Owner shall be responsible for the removal of foodstuffs from the work area.

 4. Non-related personnel in the work area shall be kept to a minimum.

* 1. WARRANTY
1. Sherwin-Williams warrants that material shipped to buyers at the time of shipment substantially free from material defects and will perform substantially to Sherwin-Williams published literature if used in accordance with the latest prescribed procedures and prior to the expiration date.
2. Sherwin-Williams liability with respect to this warranty is strictly limited to the value of the material purchase. One-year standard material warranty.

PART 2 – PRODUCTS

2.1 COATING

 A. Sherwin-Williams Resuwall VC, epoxy-based, urethane topcoat, chip seamless wall system

 1. System Materials:

 a. Broadcast Coat: Sherwin-Williams Resuflor Gard No Sag resin and hardener.

 b. Chips: Sherwin-Williams decorative chips (Micro or Macro)

 c. Grout Coat: Sherwin-Williams Resuflor Glaze resin and hardener.

 d. Topcoat: Sherwin-Williams Armor Top resin and hardener

1. Patch Materials

 a. Shallow Fill and Patching: Use Sherwin-Williams Resuflor Cove Rez.

2.2 MANUFACTURER

 A. The Sherwin-Williams High Performance Flooring, 866-540-1299 swflooring@sherwin.com Website: <https://industrial.sherwin-williams.com/na/us/en/resin-flooring.html>

 B. Manufacturer of Approved System shall be single source and made in the USA.

 C. Alternates must be approved 10 days prior to bid.

2.3 PRODUCT REQUIREMENTS

 First Broadcast Coat Resuflor Gard No Sag

 1. Percent Solids 100 %

 2. VOC 3.45 g/L

 3. Compressive Strength, ASTM D 695 16,000 psi

 4. Tensile Strength, ASTM D 638 3,800 psi

 5. Flexural Strength, ASTM D 790 4,000 psi

 6. Abrasion Resistance, ASTM D 4060

 C-10 Wheel, 1,000 gm load, 1,000 cycles 35 mg loss

 7. Flame Spread/NFPA-101, ASTM E 84 Class A

 8. Flammability, ASTM D 635 Self Extinguishing

 9. Impact Resistance MIL D-3134 0.025 inch Max

 10. Water Absorption. MIL D-3134 0.04 %

 11. Potlife @ 70 F 20-25 minutes

 Second Broadcast Coat and Grout Coat Resuflor Glaze

 1. Percent Solids 100 %

 2. VOC 3.8 g/L

 3. Compressive Strength, ASTM D 695 11,200 psi

 4. Tensile Strength, ASTM D 638 2,100 psi

 5. Flexural Strength, ASTM D 790 5,100 psi

 6. Abrasion Resistance, ASTM D 4060

 C-10 Wheel, 1,000 gm load, 1,000 cycles 29 mg loss

 7. Flame Spread/NFPA-101, ASTM E 84 Class A

 8. Impact Resistance MIL D-24613 0.0007 inches, no cracking or delamination

 9. Water Absorption. MIL D-24613 Nil

 10. Potlife @ 70 F 20 minutes

 Topcoat Resuflor Armor Top

 1. VOC 0 g/L

 2. 60 Degree Gloss ASTM D523 75+/-5

 3. Mixed Viscosity, (Brookfield 25oC) 500 cps

 4. Tensile strength, ASTM D 638 7,000 psi

 5. Abrasion Resistance, ASTM D4060 Gloss Satin

 CS 17 wheel (1,000 g load) 1,000 cycles 4 8 mg loss with grit

 10 12 mg loss without grit

 6. Pot life @ 70o F 50% RH 2 hours

 7. Dry properties, 70oF, 50% R.H. 8 hours tack free, 12 hours Dry

 60oF, 30% RH 12 hours tack free, 18 hours Dry

 80oF, 70%RH 4 hours tack free, 6 hours Dry

 8. Flash Point PMCC 186oF

 9. Full Chemical resistance 7 days

PART 3 – EXECUTION

* 1. EXAMINATION

A. Examine substrates, areas and conditions, with Applicator present, for compliance with requirements for maximum moisture content, installation tolerances and other conditions affecting coating performance.

 1. Verify that substrates and conditions are satisfactory for installation and comply with requirements specified.

3.2 PREPARATION

1. General

 1. New and existing concrete surfaces shall be free of oil, grease, curing compounds, loose particles, moss,

 algae growth, laitance, friable matter, and dirt.

 2. There shall be no visible moisture present on the surface at the time of application of the system.

1. Remove loose mortar spatter, joint compounds etc.
2. Create a surface profile on concrete with sandblasting apparatus and/or dust-free diamond grinders.
3. Masonry block shall be clean, and dry.
4. Drywall shall be completely clean and free of any oils, soap residue, gypsum dust etc.
	1. APPLICATION
5. General

 1. The system shall be applied in six distinct steps as listed below:

 a. Substrate preparation

1. Priming
2. Broadcast coat application with chip broadcast
3. Second broadcast coat application with chip broadcast
4. Grout coat application
5. Topcoat application

 2. The handling, mixing and addition of components shall be performed in a safe manner to achieve

 the desired results in accordance with the Manufacturer's recommendations.

 3. The system shall follow the contour of the substrate.

 4. A neat finish with well-defined boundaries and straight edges shall be provided by the Applicator.

.

 B. Priming

Sherwin-Williams Heavy Duty Block Filler is recommended to fill any pores in the substrate when applying over concrete or block walls. Consult Sherwin-Williams for block filler at continuous wet areas. When applying over sheet rock, prime with Sherwin-Williams Extreme Bond Primer.

 C. 1st Broadcast Coat

 1. The broadcast coat shall be Resuflor Gard No-SAG resin, and hardener.

 2. The resin shall be added to the hardener and thoroughly mixed by suitably approved mechanical means.

1. The base coat shall be applied by a roller at the rate of 200 sf/gal to yield a dry film thickness of 8 mils.
2. The chip will be broadcast into the wet resin at the rate of 0.1-0.12 lb/SF.
3. After curing remove loose chips by brushing with stiff brush

 D. 2nd Broadcast Coat

 1. A second broadcast coat will be applied as the first.

 E. Grout Coat

 1. The grout coat shall be comprised Resuflor Glaze resin, and hardener.

 2. The resin shall be added to the hardener and thoroughly mixed by suitably approved mechanical means.

3. The grout coat shall be applied using a roller at the rate of 200 sf/gal to yield a dry film thickness of

 8 mils.

 F. Topcoat

 1. The topcoat of Armor Top is typically applied using the dip and roll method at the rate of 700 sq ft /gal. Armor Top should not be applied more than 2 mils wet and must be applied twice.

 2. The topcoats shall be comprised of a liquid resin and hardener that is mixed at the ratio per the manufacturer’s instructions.

 3. The finish system will have a nominal thickness of 40 mils.

3.4 FIELD QUALITY CONTROL

 A. Tests, Inspection

 1. The following tests shall be conducted by the Applicator:

 a. Temperature

 1. Air, substrate temperatures and, if applicable, dew point.

 b. Coverage Rates

 1. Rates for all layers shall be monitored by checking quantity of material used against the area covered.

* 1. CLEANING AND PROTECTION

 A. Cure material in compliance with manufacturer’s directions, taking care to prevent their contamination during stages of application and prior to completion of the curing process.

 B. Remove masking. Perform detail cleaning to leave cleanable surface for subsequent work of other sections.

5/16/2025-Resuwall VC

*Please recycle - Thank you!*