SECTION 096723

RESINOUS FLOORING

SHERWIN-WILLIAMS HIGH PERFORMANCE FLOORING, RESUFLOR DECO QUARTZ DB23

- GENERAL

  - SECTION INCLUDES

    - Resinous Systems of the Following Types:

      - Sherwin-Williams HPF, Resuflor Deco Quartz DB23.

  - RELATED SECTIONS

    - Section 03300 – Cast-In-Place Concrete.

  - REFERENCES

    - ASTM International (ASTM):

      - ASTM C 29 / C 29M - Standard Test Method for Bulk Density ("Unit Weight") and Voids in Aggregate.

      - ASTM C 128 - Standard Test Method for Density, Relative Density (Specific Gravity), and Absorption of Fine Aggregate.

      - ASTM C 413 - Standard Test Method for Absorption of Chemical-Resistant Mortars, Grouts, Monolithic Surfacings, and Polymer Concretes.

      - ASTM C 566 - Standard Test Method for Total Evaporable Moisture Content of Aggregate by Drying.

      - ASTM D 635 - Standard Test Method for Rate of Burning and/or Extent and Time of Burning of Plastics in a Horizontal Position.

      - ASTM D 695 - Standard Test Method for Compressive Properties of Rigid Plastics.

      - ASTM D1475 - Standard Test Method For Density of Liquid Coatings, Inks, and Related Products.

      - ASTM D 2047 - Standard Test Method for Static Coefficient of Friction of Polish-Coated Flooring Surfaces as Measured by the James Machine.

      - ASTM D 2240 - Standard Test Method for Rubber Property—Durometer Hardness.

      - ASTM D 2244 - Standard Practice for Calculation of Color Tolerances and Color Differences from Instrumentally Measured Color Coordinates.

      - ASTM D2369 - Standard Test Method for Volatile Content of Coatings.

      - ASTM D 2370 - Standard Test Method for Tensile Properties of Organic Coatings.

      - ASTM D 3960 - Standard Practice for Determining Volatile Organic Compound (VOC) Content of Paints and Related Coatings.

      - ASTM D 4060 - Standard Test Method for Abrasion Resistance of Organic Coatings by the Taber Abraser.

      - ASTM D 4366 - Standard Test Methods for Hardness of Organic Coatings by Pendulum Damping Tests

      - ASTM D5441 - Standard Test Method for Analysis of Methyl Tert-Butyl Ether (MTBE) by Gas Chromatography.

      - ASTM D 7234 - Standard Test Method for Pull-Off Adhesion Strength of Coatings on Concrete Using Portable Pull-Off Adhesion Testers.

      - ASTM F 1869 - Standard Test Method for Measuring Moisture Vapor Emission Rate of Concrete Subfloor Using Anhydrous Calcium Chloride.

      - ASTM F 2170 - Standard Test Method for Determining Relative Humidity in Concrete Floor Slabs Using in situ Probes

      - ASTM G 154 - Standard Practice for Operating Fluorescent Ultraviolet (UV) Lamp Apparatus for Exposure of Nonmetallic Materials.

      - ASTM G 155 - Standard Practice for Operating Xenon Arc Light Apparatus for Exposure of Non-Metallic Materials.

    - Deutsches Institut fur Normung (DIN):

      - DIN 53460 – Testing of Plastics; Determination of the Vicat Softening Temperature of Thermoplastics.

    - International Concrete Repair Institute (ICRI):

      - ICRI 310.2R - Selecting and Specifying Concrete Surface Preparation for Sealers, Coatings, Polymer Overlays, and Concrete Repair.

    - Military Specifications (MIL):

      - MIL-D-3134J - Deck Covering Materials.

    - National Floor Safety Institute (NFSI):

      - ANSI/NFSI B101.1 - Test Method for Measuring Wet SCOF of Common Hard-Surface Floor Materials.

  - SUBMITTALS

    - Submit under provisions of Section 01300.

    - Product Data:

      - Manufacturer's data sheets on each product to be used, including properites, VOC content, wet static coefficient of friction, compressive strength, tensile strength, eloongation and similar properties.

      - Preparation instructions and recommendations.

      - Storage and handling requirements and recommendations.

      - Typical installation methods.

    - Verification Samples:  Two representative units of each system, including color and texture.

    - Shop Drawings:  Include details of materials, construction and finish. Include relationship with adjacent construction.

    - Manufacturer’s Certification:  Submit manufacturer’s certification that materials comply with specified requirements and are suitable for intended application.

    - Manufacturer’s Project References:  Submit manufacturer’s list of successfully completed resinous flooring system projects, including project name and location, name of architect, and type and quantity of flooring systems furnished.

    - Applicator’s Project References:  Submit applicator’s list of successfully completed resinous flooring system projects, including project name and location, name of architect, and type and quantity of flooring systems applied.

    - Care and Maintenance Instructions:  Submit manufacturer’s care and maintenance instructions, including cleaning instructions.

  - QUALITY ASSURANCE

    - Manufacturer Qualifications:  Company specializing in manufacturing products specified in this section with a minimum five years documented experience.

    - Applicator’s Qualifications:

      - Applicator regularly engaged, for a minimum of 5 years, in application of resinous flooring systems of similar type to that specified.

      - Employ persons trained for application of resinous flooring systems.

    - Source Limitations:  Provide each type of product from a single manufacturing source to ensure uniformity.

    - Mock-Up:  Construct a mock-up with actual materials in sufficient time for Architect’s review and to not delay construction progress. Locate mock-up as acceptable to Architect and provide temporary foundations and support.

      - Intent of mock-up is to demonstrate quality of workmanship and visual appearance.

      - If mock-up is not acceptable, rebuild mock-up until satisfactory results are achieved.

      - Retain mock-up during construction as a standard for comparison with completed work.

      - Do not alter or remove mock-up until work is completed or removal is authorized.

  - PRE-INSTALLATION CONFERENCE

    - Convene a conference approximately two weeks before scheduled commencement of the Work. Attendees shall include Architect, Contractor and trades involved. Agenda shall include schedule, responsibilities, critical path items and approvals.

  - DELIVERY, STORAGE, AND HANDLING

    - Delivery Requirements:  Deliver materials to site in manufacturer’s original, unopened containers and packaging, with labels clearly identifying product name, manufacturer, and batch number.

    - Storage and Handling Requirements:

      - Store and handle materials in accordance with manufacturer’s instructions.

      - Keep materials in manufacturer’s original, unopened containers and packaging until application.

      - Store materials in clean, dry area indoors between 65 and 80 degrees F (18 and 27 degrees C).

      - Store materials out of direct sunlight.

      - Keep materials from freezing.

      - Protect materials during storage, handling, and application to prevent contamination or damage.

  - PROJECT CONDITIONS

    - Apply flooring system under the following ambient conditions:

      - Ambient and Concrete Floor Temperatures:  Between 65 and 85 degrees F (18 and 29 degrees C).

      - Material Temperature:  Between 65 and 85 degrees F (18 and 29 degrees C).

      - Relative Humidity:  Maximum 80 percent.

      - Dew Point:  Floor temperature more than 5 degrees over dew point.

    - Do not apply flooring system under ambient conditions outside manufacturer’s limits.

  - WARRANTY

    - Submit manufacturer’s standard warranty.

- PRODUCTS

  - MANUFACTURERS

    - Acceptable Manufacturer:  The Sherwin-Williams High Performance Flooring, 866-540-1299 swflooring@sherwin.com  Website: https://industrial.sherwin-williams.com/na/us/en/resin-flooring.html

    - Requests for substitutions will be considered in accordance with provisions of Section 01600.

  - SHERWIN-WILLIAMS HPF, RESUFLOR DECO QUARTZ DB23

    - Resuflor Deco Quartz DB23.

      - First Broadcast Coat with decorative quartz broadcast:  Resuflor MPE, 10-12 mils.

      - Second Broadcast Coat with decorative quartz broadcast:  Resuflor MPE, 15 mils.

      - Grout Coat:  Resuflor UVE, 15 mils.

      - Topcoat:  Resutile HTS 100, 3 mils.

      - Color:  As selected by Architect from manufacturer's full range.

  - SYSTEM PROPERTIES

    - Tennant Quartz DB

      - Abrasion Resistance, Taber Abraser CS-17 Taber Abrasion Wheel, 1,000 gram load, 1,000 revolutions, ASTM D4060, 18 mg/loss

      - Adhesion to Concrete, psi [MPa], ASTM D4541, 450 [3.10] (concrete failed)

      - Adhesion to Concrete, psi [MPa[, ASTM D7234, 732 [4.48] (concrete failed)

      - Coefficient of Friction-COF, James Friction Tester, ASTM D2047, 0.63

      - Coefficient of Friction-Wet Static, BOT 3000, ANSI/NFSI B101.1, 0.94

      - Compressive Strength, psi [MPa], ASTM D695, 13,500 [93.079]

      - Flammabilitymm/min, ASTM D635, 182 mm/min

      - König Hardness, ASTM D22540, 171.3

      - Shore D hardness, ASTM D2240, 80-85 @ 0 sec | 75-80 @ 15 sec

      - Sward Hardness (1mil flim), ASTM D2240, 30-40

      - Tensile Strength, psi [MPa], ASTM D2370, 8,000 [55.158]

      - Percent Elongation (resin only), ASTM D2370, 6%

      - Volatile Organic Compound, VOC,lb/gal [g/l], ASTM D3960, Resuflor MPE A+B= 0.41 [49] Resuflor UVE A+B=0.67 [81] Resutile HTS 100 A+B+C=0.05 [6]

      - Water Absorption (24 hours0, ASTM D570, 0.2% weight increase

  - PRODUCT PROPERTIES

    - Resuflor MPE:  A neutral, two-component, high solids epoxy.

      - Percent Solids, by weight (by volume), ASTM D1475, A + B:  95.45 (94.56).

      - Volatile Organic Compound-VOC, ASTM D3960, Mixed A + B:  0.41 lb./gal (49 g/L).

      - Abrasion Resistance, mg loss, Taber Abraser, C-17 Taber Abrasion Wheel, 1,000 gram load, 1,000 revolutions,  ASTM D4060:  83.1.

      - Coefficient of Friction-COF, James Friction Tester, ASTM D2047:  0.59-0.62.

      - Adhesion to Concrete, ASTM D5441:  732 psi (4.48 MPa) concrete failed.

      - Adhesion to Concrete, ASTM D7234:  450 psi (3.10 MPa) concrete failed.

      - Compressive Strength, ASTM D695:  13,500 psi (93.079 MPa).

      - Tensile Strength, ASTM D2370:  8,000 psi (55.158 MPa).

      - Percent Elongation, ASTM D2370:  5.

      - Shor D Hardness, ASTM D2240:  80-85 @ 0 sec, 75-80 @ 15 sec.

    - Resuflor UVE:  A two-component, high solids, UV resistant epoxy.

      - Percent Solids, by weight (by volume), ASTM D2369, A + B:  92.60 (92.11).

      - Volatile Organic Compound-VOC, ASTM D3960, A + B:  0.67 lb./gal (81 g/L).

      - Abrasion Resistance, mg loss, Taber Abraser, C-17 Taber Abrasion Wheel, 1,000 gram load, 1,000 revolutions, ASTM D4060:  80-90.

      - Coefficient of Friction-COF, James Fricion Tester, ASTM D2047:  0.59-0.62.

      - Compressive Strength, ASTM D69:  13,500 psi (93,150 MPa).

      - Tensile Strength, ASTM D2370:  8,000 psi (55,158 MPa).

      - Present Elongation, ASTM D2370:  5.

      - Shore D Hardness, ASTM D2240:  80-85 @ 0 sec, 70-85 @ 15 sec.

    - Resutile HTS 100:  A clear high solids, three-component, satin finish, aliphatic, moisture-cure urethane.

      - Percent Solids, by weight (by volume), ASTM D2369,  A + B + C:  94.02 (92.57).

      - Volatile Organic Compound-VOC, ASTM D3960, Mixed A + B + C:  0.05 lb/gal (6 g/L).

      - Abrasion Resistance, mg loss, Taber Abraser, C-17 Taber Abrasion Wheel, 1,000 gram load, 1,000 revolutions, ASTM D4060:  18.

      - Coefficient of Friction-COF, James Friction Tester, ASTM D2047:  0.63.

      - Wet Static Coefficient of Friction, BOT 3000, ANSI/NFSI B101.1:  0.94.

      - Flammability, ASTM G154:  182 mm/min.

      - Resistance to Yellowing as measured using ASTM D2244 after 1000 consecutive hours UV exposure in QUV, ASTM G154, <10 increase of yellow units (CIE Lab Δb)

      - Tensile Strength, (resin only), ASTM D2370: 6,250 psi (43,092 MPa).

      - Percent Elongation, (resin only), ASTM D2370: 6.

      - König Hardness, (3 mil/76.2 micron film), ASTM D4366: 171.3.

      - Water Absorption, 24-hour immersion, ASTM C413: 0.2 percent weight increase.

      - Color:  Selected by Architect.

    - Decorative Quartz (Broadcast):  Description, Color-coated, uniformly shaped and sized quartz granules

      - Grain Size:  40 mesh.

      - Mohs Hardness:  6.5-7.

      - Bulk Density, ASTM C29, packed:  90-105 pcf.

      - Specific Gravity, ASTM C128:  2.65.

      - Moisture Content, ASTM C566:  Less than 0.05 percent.

      - Colorfastness/UV Stability, ASTM G155:  1,000 hours, pass.

      - Color:  Selected by Architect.

- EXECUTION

  - EXAMINATION

    - Examine concrete surfaces to receive flooring system.  Verify concrete is structurally sound.

    - Moisture Testing of Concrete:  Perform at least one of the following two tests to determine moisture in concrete.  Type of test and frequence as recommended by manufacturer and installer.

      - In-situ Probe Test:

        - Measure relative humidity in concrete in accordance with ASTM F 2170.

        - Application of flooring system shall start only if test results are below 75 percent relative concrete humidity.

        - If test results are above limits, notify Architect and flooring manufacturer in writing.

    - Do not begin preparation or installation until satisfatory moisture test results are achieved.  Provide flooring manufacturer's recommended moisture vapor control coating if required.

  - PREPARATION

    - Clean surfaces thoroughly prior to installation.

    - Protection of In-Place Conditions:  Protect adjacent surfaces and adjoining walls from contact with flooring system materials.

    - Surface Preparation:

      - Prepare concrete surface in accordance with manufacturer’s instructions.

      - Remove dirt, dust, debris, oil, grease, curing agents, bond breakers, paint, coatings, sealers, silicones, and other surface contaminants which could adversely affect application of flooring system.

      - Steel shot blast concrete to a minimum surface profile of ICRI 310.2R, CSP 5.

      - Key-cut termination points with 1/4-inch (6-mm) by 1/4-inch (6-mm) cut.

      - Patch depressions, divots, and cracks in concrete in accordance with manufacturer’s instructions.

      - Mechanically remove loose, delaminated, and damaged concrete and repair in accordance with manufacturer’s instructions.

      - Joints:  Fill joints in accordance with manufacturer’s instructions.

  - INSTALLATION

    - Install flooring system in accordance with manufacturer’s instructions and approved submittals at locations indicated on the Drawings.

    - Ensure concrete is dry, clean, and prepared in accordance with manufacturer’s instructions.

    - Allow concrete to cure a minimum of 7 days before applying flooring system.

    - Mixing:

      - Mix material components together in accordance with manufacturer’s instructions.

      - Mix only enough material that can be applied within working time.

      - Add and mix colorants with materials in accordance with manufacturer’s instructions to achieve uniform color.

    - Apply flooring system materials to obtain consistent mil thickness and smooth, uniform appearance and texture.

    - Overlay:  Apply overlay in accordance with manufacturer’s instructions.  Apply overlay to prepared concrete surface.

    - Traction Aggregate:  Broadcast traction aggregate in accordance with manufacturer’s instructions.  Broadcast traction aggregate into wet overlay.

    - Cove:

      - Apply cove primer and cove in accordance with manufacturer’s instructions at locations indicated on the Drawings.

      - Apply cove to height and shape as indicated on the Drawings.

      - Apply cove to create seamless, smooth transition between flooring and walls.

    - Seal Coat:

      - Apply seal coat in accordance with manufacturer’s instructions.

      - Apply seal coat over traction aggregate.

  - FIELD QUALITY CONTROL

    - Field Inspection:  Coordinate field inspection in accordance with appropriate sections in Division 01.

    - Manufacturer’s Services:  Coordinate manufacturer’s services in accordance with appropriate sections in Division 01.

  - CLEANING AND PROTECTION

    - Allow flooring system to dry in accordance with manufacturer’s instructions before opening to traffic.

    - Allow flooring system to dry a minimum of 1 week before cleaning by mechanical means.

    - Protect completed flooring system from damage during construction.

END OF SECTION